## Slide 1: Chemical and Physical Properties
MFG 355

## Slide 2: Level of focus – Macrostructures
Chemical and Physical properties
  UV stability
  Oxidation stability
  Plasticization
  Adhesive bondability
  Diffusion
  Flammability
  Optical properties
  Conductivity

## Slide 3: What Determines Chemical and Physical Properties?
Polarity of atoms within the polymer molecules
Size of the crystal structures within resin
Space between the polymer molecules
Presence of additives
Ability of the electrons to move freely within the molecules
Chemical reactivity of atoms within the polymer molecules

## Slide 4: Resin Rules
Resin Rules: UV and oxidation combine in degradation of plastics.
  UV and oxidative degradation are also called weathering
  Unsaturation and aromatic have poor UV and oxidative resistance
  Coatings can protect from weathering but they also are attacked eventually

## Slide 5: Ultraviolet (UV) Light Degradation

## Slide 6: Oxidation
Plastic paint

## Slide 7: Weathering
Prevention or reduction of weathering
  UV absorbers
    Complex organic molecules
    Carbon black
  UV blockers
    Pigments (especially titanium dioxide) (paint)
  Anti-oxidants
    Typical concentrations = 1-2%

## Slide 8: Coatings
Decorative and protective
  Adhesion
  Weatherability

## Slide 9: Environmental Resistance and Weathering

## Slide 10: Resin Rules
Resin Rules: Many polymers will form cracks when under stress.
  Stress cracks are accelerated by environmental conditions
  Stress cracks are accelerated by temperature
  Stress cracks are accelerated by crystallinity
  Stress cracks are accelerated by internal stress areas
  Stress cracks are accelerated by molecular alignment

## Slide 11: Environmental Stress Cracking
Hawaii Story
  Crosslinked, LLDPE
Banana Plantation
  Drawdown

## Slide 12: ESCR
Bottles in Utah
  Fertilizer
  Thickest part of the bottle

## Slide 13: Crazing
Cracks at stress areas

## Slide 14: Resin Rules
Resin Rules: Solvent attack on plastics depends on polarity, shape, openness and chemical reactivity.
  Polarity effect follows like-with-like
  Shape effect follows size interference
  Openness effect follows crystallinity and size interference
  Chemical reactivity depends on chemical groups

## Slide 15: Chemical resistivity and solubility
None
Swelling/softening
Dissolving
Reacting
PE and H2O
Nylon and H2O
PVC and ketone
PVOH and water
Cellulosics
and acids
Increasing Chemical Reactivity to Plastic

## Slide 16: Chemical Resistivity and Solubility
PS exposed to gasoline
  Chemical reactivity

## Slide 17: Chemical Nature and Solvent-Solute Interactions
Nylon water heater
  Polar
  Internal stresses
  Thermal
Nylon in hot water

## Slide 18: Plasticizers (Solvents)
Increase swelling
  Randomness
Plasticizers can migrate out

## Slide 19: Thermodynamics of Solvent Interactions
ΔG = ΔH – TΔS (Free Energy Equation)
    ΔG is free energy and the reaction (solvation) will occur when ΔG is negative
    ΔH is enthalpy (energy content of bonds) and gets negative when bonds are formed (more stable)
    ΔS is entropy and is positive when randomness increases
  When does each variable contribute to a negative ΔG (thermodynamically favoring solvation)?
    When ΔH is highly negative (formation of many bonds)
    When ΔS increases greatly (increasing randomness)
    When T becomes large (high temperature)

## Slide 20: Adhesive and Solvent Welding
PVC adhesive
  Adhesive solvent reacts with the surface
  Solvent dries leaving polymer layer in the interphase
Solvent welding
  Softens the surface and then evaporates as the surfaces are pressed together (creating an entangled interphase)

## Slide 21: Water Repellent
Surface energy must be LOW
  PTFE = 20 mN/m (lowest plastic)
  PE = 35 mN/m (moderate)
  PVC = 41.5 mN/m (fairly high)
  Nylon = 46.5 mN/m (high)
  Copper = 165 mN/m (very high – typical metal)

## Slide 22: Corrosion-Resistant
Availability of electrons
Polymers are better than metals
Fluoropolymers—tightly attached
Solvent effects are much more important in plastics than are corrosion effects

## Slide 23: Resin Rules
Resin Rules: While all plastics are more permeable that most metals and ceramics, permeability depends on the plastic.
  Thickness decreases permeability
  Crystallinity decreases permeability
  Branching and large pendant groups open the structure and increase permeability
  Polar attractions between the polymer and the gas increase permeability

## Slide 24: Gas (vapor) Permeation
Polar groups (solubility) to solvent or gas
Intermolecular size (distance)
Crosslinking and crystallinity

## Slide 25: Permeability
Wide range of values
  16 orders of magnitude at a single temperature
Diffusion Coefficient
  D = Doe-A/RT
Fick’s Laws of diffusion
  J = -D dc/dx
Barrier Properties
  dc/dt = D d2c/dx2

## Slide 26: Resin Rules
Resin Rules: Electrical activity depends on the ability of the electrons to move within the polymer.
  Polymers generally have poor conductivity because the electrons are locked (shared) between atoms
  Recent advances in polymer chemistry have developed de-localized electrons

## Slide 27: Electrical Properties
Resistivity (1018 – 10-6)
Dielectric Strength
Arc Resistance
Dielectric Constant
Dissipation Factor (heat up)

## Slide 28: Conductive Polymers

## Slide 29: Conductive Polymers
Material | Conductivity (Ohm-cm)-1
Silver | 6.25 x 105
Copper | 5.85 x 105
Gold | 4.44 x 105
Polyacetylene (doped) | 6.0 x 104 - 1.5 x 105
Steel | 6.0 x 104
Silicon | 1.56 x 10-3
Carbon, graphite | 1.0 x 10-3
Polyacetylene (unmodified) | 1.0 x 10-11 to .1.0 x 10-15
Carbon, diamond | 1.0 x 10-14
Alumina ceramic | 1.0 x 10-15
Epoxy | 1.0 x 10-15
Polyethylene, medium density | 1.0 x 10-16
Teflon | 1.0 x 10-18

## Slide 30: Resin Rules
Resin Rules: Optical properties depend upon the ability of light to pass through the polymer.
  Crystallinity decreases clarity
  Multiple phases decrease clarity
  Light refraction decreases clarity

## Slide 31: Optical Properties
Light Transmission
  Clear
  Translucent
  Opaque

## Slide 32: Optical Properties
Colorants
  Dyes
  Pigments

## Slide 33: Transparency
Non-crystalline
  PET is exception because of size of the crystals
Index of refraction – low
Total luminous transmittance – high

## Slide 34: Resin Rules
Resin Rules: Polymer flammability depends on the basic thermal stability and the ability to char or smother the flame.
  High aromatic raises thermal stability
  High aromatic content increases char
  Halogen content smothers flames but increases smoke toxicity
  Water vapors (usually in fillers) smother flame

## Slide 35: Flammability
Self-extinguishing
  Halogen effects (oxygen)
  Fillers (Al2O3·3H2O) (heat)
  Aromatics (fuel)
  Silicones (fuel)
Fuel
Oxygen
Heat

## Slide 36
Flammability of aircraft seats with PBI foam
PBI foam
Conventional foam

## Slide 37: Resin Rules
Resin Rule: The charring property of some resins can be used to produce a material that has extremely high thermal stability.
  The charring step is usually done in a oxygen-free (or low oxygen) environment.
  These resins require multiple charring/infusion steps to minimize the void content.
  When reinforced with carbon fibers, the material is both thermally stable and strong.

## Slide 38
Rocket Exit Throat
Exit Nozzle
(Ablative
Material)
10 oF
500 oF
4000 oF
Rocket
Motor
Rocket
Propellant
Nose
Cone
Rocket exit nozzle with phenolic as the ablative material

## Slide 39: Flammability Tests
Vertical and horizontal burn tests

## Slide 40
Limiting Oxygen Index
Chamber
Sample
Sample holder
Gas manifold
N2
O2

## Slide 41: Flammability Tests
Radiant panel
Cone calorimeter

## Slide 42: Heat Resistance
Stiffening groups along the chain
  Tg goes up since it takes more heat to move molecules
  Phenyl groups
Strong intermolecular H-bonding increases heat resistance
Crystallinity increases heat resistance

## Slide 43: Insulating Polymers
Non-polar is better
  Movement of molecules absorbs energy
Foams
  Air is an insulator

## Slide 44: Resin Rules
Resin Rules: Plastics are identified by their chemical and physical properties.
  Chemical groups are detected by FTIR
  Physical properties include: smoke, light transmission, melting point, solvent sentivity

## Slide 45: Plastic Identification
Spectroscopy (FTIR)

## Slide 46: Thank You