## Slide 1: Designing with Plastics
MFG 355

## Slide 2: Design Methodology
Inspiration
Concept
Prototype
Development
Final product

## Slide 3: How to get Inspiration
It’s all in how you think

## Slide 4: How to get inspiration
Logical thinking
Intuitive thinking

## Slide 5: First Step in Concept: Layout or Drawing
Sketch
Drawing
CAD
Advantages and disadvantages to each
  Detail
  Complexity
  Time
  Communication of idea
  Visualization of problems

## Slide 6: Second Step in Concept: Constraints
Appearance
Mechanical
Environmental
Safety, Codes and Standards
Manufacturing Method/Design Rules
Economics

## Slide 7: Third Step in Concept: Material Choice
Database – IDES (like in lab) or others
  Multiple grades
    Multiple additives
    Multiple blends

## Slide 8: Material Choice
Selection methodology
  Define the criteria for material selection
  Determine the advantages and disadvantages of each polymer type
  Select polymers for special properties
  Rank the resins and make a preliminary selection
Computer-aided selection

## Slide 9: Material Selection Matrix
Resins | Properties |  |  |  |  |  |  |  | 
 | Property 1: |  | Property 2: |  | Property 3: |  | Property 4: |  | 
 | Value/Rank | WF= | Value/Rank | WF= | Value/Rank | WF= | Value/Rank | WF= | Total Score
 |  | Score |  | Score |  | Score |  | Score | 

## Slide 10: Material Selection
Choosing material for a snow sled

## Slide 11: PLASTICS HAVE FOLLOWED A CONSISTENT PATTERN OF APPLICATION GROWTH
Enabler applications
Platform application
Widespread substitution
  Simple, new applications in which the plastic allows people to do things they couldn’t do before
  Single major application in which the plastic replaces incumbent material based on superior properties
  Material competes with incumbent materials in many applications based on performance and cost
Description
Purpose
Typical timeframe
Source: Modern Plastics, team analysis
  Build credibility, capability, knowledge, and awareness around material
  Establish commercial viability of material
  Generate first profits
  Generate long term volume and profits for material
  First 2-3 years after commercialization (full scale production)
  2-6 years after commercialization
  6+ years after commercialization

## Slide 12: Material Choice ― Cost/Performance
Cost/Performance
Amorphous
Semi-crystalline
High
Performance
Polymers
Mid-Range
Polymers
Common
Polymers
PS
SAN
PVC
LDPE
HDPE
PP
PE-UHMW
POM
PBT
PET
PA-6/6,6
PA-4,6
PPA
PPS
LCP
PVDF
FP
PEEK
PI
PAI
TPI
PPSU
PEI
PES
PSF
PAR
PPC
PC
PPO
SMA
ABS
PMMA
ABS-acrylonitrile butadiene styrene
FP-fluoropolymers
HDPE-high density polyethylene
LCP-liquid crystal polymers
LDPE-low density polyethylene
PA 4,6-polyamide 4,6
PA 6/6,6-polyamide 6/6,6
PAI-polyamide imide
PAR-polyarylate
PBT-polybutylene terephthalate
PC-polycarbonate
PE UHMW-ultrahigh mol. weight PE
PEEK-polyetheretherketone
PEI-polyether imide
PES-polyethersulfome
PET-polyethylene terephthalate
PI-polyimide
PMMA-polymethyl methacrylate
POM-polyoxymethylene
PP-polypropylene
PPA-polyphtalamide
PPC-polyphthalate carbonate
PPO-polyphenylene oxide
PPS-polyphenylene sulfide
PPSU-polyphenylsulfone
PS-polystyrene
PSF-polysulfone
PVC-polyvinyl chloride
PVDF-polyvinylidene fluoride
SAN styrene acrylonitrile
SMA-styrene maleic anhydride
TPI-thermoplastic polyimide

## Slide 13: Material Selection Matrix
Resins | Properties |  |  |  |  |  |  |  | 
 | Property 1: |  | Property 2: |  | Property 3: |  | Property 4: |  | 
 | Value/Rank | WF= | Value/Rank | WF= | Value/Rank | WF= | Value/Rank | WF= | Total Score
 |  | Score |  | Score |  | Score |  | Score | 
HDPE |  |  |  |  |  |  |  |  | 
LDPE |  |  |  |  |  |  |  |  | 
ABS |  |  |  |  |  |  |  |  | 
PC |  |  |  |  |  |  |  |  | 
PS |  |  |  |  |  |  |  |  | 
PP |  |  |  |  |  |  |  |  | 
Choosing material for a snow sled
Possible resins

## Slide 14: Material Selection Matrix
Resins | Properties |  |  |  |  |  |  |  | 
 | Property1: Toughness |  | Property 2: Abrasion Resist |  | Property 3: Surface Finish |  | Property 4: Cost |  | 
 | Value/Rank | WF= | Value/Rank | WF= | Value/Rank | WF= | Value/Rank | WF= | Total Score
 |  | Score |  | Score |  | Score |  | Score | 
HDPE |  |  |  |  |  |  |  |  | 
LDPE |  |  |  |  |  |  |  |  | 
ABS |  |  |  |  |  |  |  |  | 
PC |  |  |  |  |  |  |  |  | 
PS |  |  |  |  |  |  |  |  | 
PP |  |  |  |  |  |  |  |  | 
Choosing material for a snow sled
Desired properties

## Slide 15: Material Selection

## Slide 16: Material Selection Matrix
Resins | Properties |  |  |  |  |  |  |  | 
 | Property1: Toughness |  | Property 2: Abrasion Resist |  | Property 3: Surface Finish |  | Property 4: Cost |  | 
 | Value/Rank | WF= 5 | Value/Rank | WF= 5 | Value/Rank | WF= 3 | Value/Rank | WF= 4 | Total Score
 |  | Score |  | Score |  | Score |  | Score | 
HDPE | 4 |  | 3 |  | 1 |  | 5 |  | 
LDPE | 2 |  | 6 |  | 1 |  | 6 |  | 
ABS | 5 |  | 4 |  | 1 |  | 2 |  | 
PC | 6 |  | 2 |  | 1 |  | 1 |  | 
PS | 1 |  | 1 |  | 1 |  | 3 |  | 
PP | 3 |  | 5 |  | 1 |  | 4 |  | 
Choosing material for a snow sled
Values rank
from properties
(Higher is better)

## Slide 17: Material Selection Matrix
Resins | Properties |  |  |  |  |  |  |  | 
 | Property1: Toughness |  | Property 2: Abrasion Resist |  | Property 3: Surface Finish |  | Property 4: Cost |  | 
 | Value/Rank | WF= 5 | Value/Rank | WF= 5 | Value/Rank | WF= 3 | Value/Rank | WF= 4 | Total Score
 |  | Score |  | Score |  | Score |  | Score | 
HDPE | 4 | 20 | 2 | 10 | 1 | 3 | 5 | 20 | 
LDPE | 2 | 10 | 6 | 30 | 1 | 3 | 6 | 24 | 
ABS | 5 | 25 | 4 | 20 | 1 | 3 | 2 | 8 | 
PC | 6 | 30 | 3 | 15 | 1 | 3 | 1 | 4 | 
PS | 1 | 5 | 1 | 5 | 1 | 3 | 3 | 12 | 
PP | 3 | 15 | 5 | 25 | 1 | 3 | 4 | 16 | 
Choosing material for a snow sled
Score = value x WF

## Slide 18: Material Selection Matrix
Resins | Properties |  |  |  |  |  |  |  | 
 | Property 1:Toughness |  | Property 2: Abrasion Resist |  | Property 3: Surface Finish |  | Property 4: Cost |  | 
 | Value/Rank | WF= 5 | Value/Rank | WF= 5 | Value/Rank | WF= 3 | Value/Rank | WF= 4 | Total Score
 |  | Score |  | Score |  | Score |  | Score | 
HDPE | 4 | 20 | 2 | 10 | 1 | 3 | 5 | 20 | 53
LDPE | 2 | 10 | 6 | 30 | 1 | 3 | 6 | 24 | 67
ABS | 5 | 25 | 4 | 20 | 1 | 3 | 2 | 8 | 56
PC | 6 | 30 | 3 | 15 | 1 | 3 | 1 | 4 | 52
PS | 1 | 5 | 1 | 5 | 1 | 3 | 3 | 12 | 25
PP | 3 | 15 | 5 | 25 | 1 | 3 | 4 | 16 | 59
Choosing material for a snow sled
Total Score

## Slide 19: Material Selection Matrix
Resins | Properties |  |  |  |  |  |  |  | 
 | Property 1:Toughness |  | Property 2: Abrasion Resist |  | Property 3: Surface Finish |  | Property 4: Cost |  | 
 | Value/Rank | WF= 5 | Value/Rank | WF= 5 | Value/Rank | WF= 3 | Value/Rank | WF= 4 | Total Score
 |  | Score |  | Score |  | Score |  | Score | 
HDPE | 4 | 20 | 2 | 10 | 1 | 3 | 5 | 20 | 53
LDPE | 5 | 25 | 6 | 30 | 1 | 3 | 6 | 24 | 67
ABS | 2 | 10 | 4 | 20 | 1 | 3 | 2 | 8 | 56
PC | 1 | 5 | 3 | 15 | 1 | 3 | 1 | 4 | 52
PS | 6 | 30 | 1 | 5 | 1 | 3 | 3 | 12 | 25
PP | 3 | 15 | 5 | 25 | 1 | 3 | 4 | 16 | 59
Choosing material for a snow sled
Selecting the best

## Slide 20: Prototyping
Traditional

## Slide 21: Rapid Prototyping

## Slide 22: Prototyping
Rapid prototyping
  Stereolithography

## Slide 23: Prototyping
Rapid prototyping
  3D printing

## Slide 24: 3-D Printing

## Slide 25: Prototyping
Rapid prototyping
  Laminated object manufacturing (LOM)

## Slide 26: Prototyping
Rapid prototyping
  Selective Laser Sintering (SLS)

## Slide 27: Laser Sintering

## Slide 28: Prototyping
Rapid prototyping
  Fused deposition modeling (FDM)

## Slide 29: Prototyping
Rapid prototyping
  Fused deposition modeling (FDM)

## Slide 30: Process Selection
Some parts are more suited for a particular process
Many parts can be modified and processed through different methods
Some processes are incapable of producing certain features
  Injection molding—hollow features
  Roto-molding—deep ribs

## Slide 31: Process Selection Matrix
Processes | Features |  |  |  |  |  |  |  | 
 | Feature 1: |  | Feature 2: |  | Feature 3: |  | Feature 4: |  | 
 | Value/ Rank | WF= | Value/Rank | WF= | Value/Rank | WF= | Value/ Rank | WF= | Total Score
 |  | Score |  | Score |  | Score |  | Score | 

## Slide 32: Process Selection Matrix
Process selection for a plastic pallet

## Slide 33: Process Selection Matrix
Process selection for a plastic pallet
Processes | Features |  |  |  |  |  |  |  | 
 | Feature 1: |  | Feature 2: |  | Feature 3: |  | Feature 4: |  | 
 | Value/Rank | WF= | Value/Rank | WF= | Value/ Rank | WF= | Value/Rank | WF= | Total Score
 |  | Score |  | Score |  | Score |  | Score | 
Injection molding |  |  |  |  |  |  |  |  | 
Thermo-forming |  |  |  |  |  |  |  |  | 
Roto-molding |  |  |  |  |  |  |  |  | 
Casting/ Foaming |  |  |  |  |  |  |  |  | 
Extrusion |  |  |  |  |  |  |  |  | 
Possible
processes

## Slide 34: Process Selection Matrix
Process selection for a plastic pallet
Processes | Features |  |  |  |  |  |  |  | 
 | Feature 1: Ribs |  | Feature 2: Net shape/no assembly |  | Feature 3: Short Cycle Time |  | Feature 4: Size |  | 
 | Value/Rank | WF= | Value/Rank | WF= | Value/Rank | WF= | Value/Rank | WF= | Total Score
 |  | Score |  | Score |  | Score |  | Score | 
Injection molding |  |  |  |  |  |  |  |  | 
Thermo-forming |  |  |  |  |  |  |  |  | 
Roto-molding |  |  |  |  |  |  |  |  | 
Casting/ Foaming |  |  |  |  |  |  |  |  | 
Extrusion |  |  |  |  |  |  |  |  | 
Features

## Slide 35: Process Selection Matrix
Process selection for a plastic pallet
Processes | Features |  |  |  |  |  |  |  | 
 | Feature 1: Ribs |  | Feature 2: Net shape/no assembly |  | Feature 3: Short Cycle Time |  | Feature 4: Size |  | 
 | Value/Rank | WF= 4 | Value/Rank | WF= 3 | Value/Rank | WF= 5 | Value/Rank | WF= 6 | Total Score
 |  | Score |  | Score |  | Score |  | Score | 
Injection molding |  |  |  |  |  |  |  |  | 
Thermo-forming |  |  |  |  |  |  |  |  | 
Roto-molding |  |  |  |  |  |  |  |  | 
Casting/ Foaming |  |  |  |  |  |  |  |  | 
Extrusion |  |  |  |  |  |  |  |  | 
Weighting Factor
(higher is more
Important)

## Slide 36: Process Selection Matrix
Process selection for a plastic pallet
Processes | Features |  |  |  |  |  |  |  | 
 | Feature 1: Ribs |  | Feature 2: Net shape/no assembly |  | Feature 3: Short Cycle Time |  | Feature 4: Size |  | 
 | Value/Rank | WF= 4 | Value/Rank | WF= 3 | Value/Rank | WF= 5 | Value/Rank | WF= 6 | Total Score
 |  | Score |  | Score |  | Score |  | Score | 
Injection molding | 5 | 20 | 3 | 9 | 5 | 25 | 2 | 12 | 
Thermo-forming | 1 | 4 | 2 | 6 | 2 | 10 | 4 | 24 | 
Roto-molding | 2 | 8 | 5 | 15 | 1 | 5 | 5 | 30 | 
Casting/ Foaming | 4 | 16 | 4 | 12 | 3 | 15 | 3 | 18 | 
Extrusion | 3 | 12 | 1 | 3 | 4 | 20 | 1 | 6 | 
Score–assessment
(higher is better)

## Slide 37: Process Selection Matrix
Process selection for a plastic pallet
Processes | Features |  |  |  |  |  |  |  | 
 | Feature 1: Ribs |  | Feature 2: Net shape/no assembly |  | Feature 3: Short Cycle Time |  | Feature 4: Size |  | 
 | Value/Rank | WF= 4 | Value/Rank | WF= 3 | Value/Rank | WF= 5 | Value/Rank | WF= 6 | Total Score
 |  | Score |  | Score |  | Score |  | Score | 
Injection molding | 5 | 20 | 3 | 9 | 5 | 25 | 2 | 12 | 66
Thermo-forming | 1 | 4 | 2 | 6 | 2 | 10 | 4 | 24 | 44
Roto-molding | 2 | 8 | 5 | 15 | 1 | 5 | 5 | 30 | 58
Casting/ Foaming | 4 | 16 | 4 | 12 | 3 | 15 | 3 | 18 | 61
Extrusion | 3 | 12 | 1 | 3 | 4 | 20 | 1 | 6 | 41
Total score
(higher is better)

## Slide 38: Process Selection Matrix
Process selection for a plastic pallet
Processes | Features |  |  |  |  |  |  |  | 
 | Feature 1: Ribs |  | Feature 2: Net shape/no assembly |  | Feature 3: Short Cycle Time |  | Feature 4: Size |  | 
 | Value/Rank | WF= 4 | Value/Rank | WF= 3 | Value/Rank | WF= 5 | Value/Rank | WF= 6 | Total Score
 |  | Score |  | Score |  | Score |  | Score | 
Injection molding | 5 | 20 | 3 | 9 | 5 | 25 | 2 | 12 | 66
Thermo-forming | 1 | 4 | 2 | 6 | 2 | 10 | 4 | 24 | 44
Roto-molding | 2 | 8 | 5 | 15 | 1 | 5 | 5 | 30 | 58
Casting/ Foaming | 4 | 16 | 4 | 12 | 3 | 15 | 3 | 18 | 61
Extrusion | 3 | 12 | 1 | 3 | 4 | 20 | 1 | 6 | 41
The best

## Slide 39: Unique Product
Design example

## Slide 40: 3M Comply Product
Plastic Sheet (PE)
Covered with adhesive
Embossed Sheet (ribs connecting to edges)
Depressions filled with glass spheres
Multiply embossed sheet creating ridges and lands
Graphic film applied
Separated plastic sheet
Separated graphic product

## Slide 41: Avery-Dennison EZ Film
Plastic Sheet (PE)
Polyurethane printed cured forms (array)
Polyurethane forms pressed into the PE sheet
(thereby forming depressions and embossing the sheet)
PE sheet embossed with ridges and lands
Adhesive added
Graphic film applied
Separated graphic product
Separated embossed PE sheet

## Slide 42: 3M v. Avery-Denison
Separated plastic sheet
Separated graphic product
Separated graphic product
Separated embossed PE sheet

## Slide 43: Patent Case Decision
Avery-Dennison EZ Film
Question: Do the dots form a “regular array”
as required in the 3M patent?

## Slide 44: Thank You