## Slide 1: Commodity Resins
MFG 355

## Slide 2: Commodity Plastics
Followed a consistent price-volume curve
After maturity, price tracks the crude oil price
Products are purchased based on price or service rather than properties

## Slide 3: Polyethylene (PE)
Mer unit
Polymer chain

## Slide 4: Polyethylene
LDPE
  High Pressure/High Temperature processing
  Branching, flexibility
HDPE
  Ziegler-Natta catalyst
  Little branching
  Highly crystalline
LLDPE
  “Copolymer”—side chains prevent crystalization
  Improved toughness, strength, ESCR
UHMWPE
  Not melt processable
Crosslinked PE

## Slide 5: Polyethylene processes
High Pressure Process (LDPE)
Pressures around 350 MPa
Temp. 300ס C
Long construction lead time
Mammoth space requirements
Huge capital outlay
High energy demands
Limited to low density polyethylene
Costly and complex maintenance
Production rates vary with PE grade
Meets environmental requirements with difficulty
Rapidly inflating operating costs
Limited catalyst system choice
Catalyst removal required
Acceptable resin properties
Low Pressure Process (LLDPE)
Pressures around 3 MPa
Temp. 100ס C
Reduced const. lead time by 8-12 months
Occupies 1/10 the space
Capital outlay reduced by 50%
Reduced energy demands by 75%
Produces both HDPE and LLDPE
Easy to maintain
Same production rate for all resin grades
Environmental pollution minimal
Operating costs reduced
Several available catalysts
Catalyst removal not needed
Superior resin properties

## Slide 6: Polyethylene Properties
Relatively soft, flexible and waxy like
  Relatively low strength and stiffness
High elongation (but not elastomeric)
Easy to mold/extrude
Easy to recycle
Low surface energy (difficult to bond to)
Excellent insulation properties
Excellent solvent resistance
Low cost

## Slide 7: Polyethylene Non-woven
Different molecular weights of PE
  Different melting points
  Lay down in a mat
  Calendar at temperature between the melting points of the two materials

## Slide 8: Polyethylene Copolymer
Types of Copolymers
  Random
  Regular
  Segment/
  block
  Graft

## Slide 9: Polyethylene Copolymers
Ethylene/Vinyl Acetate (EVA)
  Glue, soft
  EVA allows water softening
Ethylene/Acrylic Acid (EAA)
  Ionic crosslinks (broken with heat)
  Tougher, stronger
  Ionomer (Surlyn)
EPM (EPDM with butadiene)
  Rubbery
  Crosslinked lightly

## Slide 10: Forms of other polyolefins

## Slide 11: Polypropylene (PP)
Mer unit
Polymer chain

## Slide 12: Polypropylene
Analogy
  I need 6 volunteers to come up front

## Slide 13: Stereoisomers of Polypropylene
Atactic (no order)
Syndiotactic (alternating order)
Isotactic (same order)
Isotactic (same order) showing methyl groups

## Slide 14: Polypropylene
Zigler-Natta catalyst
  Isotactic
  Only commercial type of polypropylene
Karl Ziegler
Guilio Natta

## Slide 15: Polypropylene Properties
Properties (compared to polyethylene)
  Similar in electrical, bonding, solvent resistance
  Stiffer
  Improved Environmental Stress Crack Resistance
  Worse UV sensitivity
  Higher Tg
  Better resistance to mechanical stress cracking
    Carpets
    Living hinges

## Slide 16: Polypropylene
Curv – Self-reinforcing composite
  Make fibers and draw to crystallize
  Crystalline areas have higher melting point
  Calendar at a temperature between the amorphous and crystalline temperatures
  Amorphous becomes the matrix for the fibers

## Slide 17: Polyvinylchloride (PVC)
Mer unit
Polymer chain

## Slide 18: PVC
Rigid
  Amorphous
  Heat sensitive (yellow)
  Often highly filled (cost)
  Solvent sensitive
    Gluing

## Slide 19: PVC
Plasticized PVC (called vinyl)
  Processed w/o heat when possible

## Slide 20: PVC
Properties
  UV sensitive
  Non-flammable (except plasticized)
    Self extinguishing
PVC
LDPE

## Slide 21: Polystyrene (PS)
Mer unit
Polymer chain

## Slide 22: Polystyrene
Non-crystalline (pendant group interference)
So what is “crystalline polystyrene”?

## Slide 23: Polystyrene Properties
Brittle and Hard
  Fair scratch resistance
  Very low price
  Very easy to mold

## Slide 24: Properties
Clear but yellows and embrittles

## Slide 25: Properties
Modified for toughness
  Impact polystyrene contains rubber

## Slide 26: PS
Foam
  expanded

## Slide 27: Copolymers, Alloys and Blends
Mixing monomers = copolymer
Mixing polymers or a polymer with a monomer (one phase) = alloy
Mixing polymers (multi-phase) = blend
Can be copolymers, alloys or blends
  HIPS (rubber added)
  SAN
  ABS

## Slide 28: ABS
PolyButadiene Rubber
PolyStyrene
A
B
S
PolyAcrylonitrile
Properties of the ABS dependant on the mix ratio
Alloys can acquire the properties of their component parts

## Slide 29: ABS

## Slide 30: Thank You