## Slide 1: Engineering and High Performance Thermoplastics
MFG 355

## Slide 2: Engineering/High Performance Thermoplastics
Replace metallic parts
  Strength and stiffness
  Retention of properties over range of temperatures
  Toughness to withstand incidental damage
  Dimensional stability
    Low creep
    Low CTE
  Withstand environmental factors (UV, O2, chemicals)
  Shaped easily compared to metals

## Slide 3: Engineering Thermoplastics
Compared to commodity plastics
  More expensive
  The commodity resins are all lacking some critical property
  Some Engineering/High Performance Thermoplastics are formed through the condensation polymerization process

## Slide 4: Polyamides or Nylons (PA)

## Slide 5: Polyamides or Nylons (PA)
( )n
[ ]a
[ ]b
[ ]a
[ ]b
Amide group
Types of nylons

## Slide 6: Types of nylons
Used to designate different a and b values which came from different monomers
  Nylon a/(b+2)
    To account for the carbons in the acid groups
  Example: Nylon 6/6
  Example: Nylon 6/12
( )n
[ ]a
[ ]b

## Slide 7: Types of nylons
What happens as a and b increase?
  More CH2 groups give greater flexibility
  More CH2 groups give more “oil-like” properties
  Fewer CH2 groups (more amide groups) gives more polarity and more strength
( )n
[ ]a
[ ]b

## Slide 8: PA General Family Characteristics
Polarity
Crystallinity
Sharp melting point
Strength
Some water absorption (depends on a/b number)

## Slide 9: PA General Family Characteristics
Highly crystalline
  Sharp melting point
Strength (polar bonding and crystallinity)
Transparent (barely)—cook-in-bag (turkey)
Anti-friction—not like PTFE but good
Toughness—excellent
Fatigue resistance—excellent
Water absorption—0.2-2.5% (must be dried for injection molding)

## Slide 10: Nylon 6/6 Monomer
Hexamethylenediamine
(6 carbons)

## Slide 11: Nylon 6/6 Monomer
Adipic Acid
(6 carbons)

## Slide 12: Nylon 6/6 Polymer
Water
Amide group

## Slide 13: Nylon 6 Monomer
Amine
Group
Acid
Group

## Slide 14: Nylon 6 Polymer
Amide group

## Slide 15: Properties of Specific Nylon Types
Nylon 6,6 – General
Nylon 6 – Copycat
Nylon 6,10 – Less water absorption
Nylon 6,12 – Flexibility and less water (silky)
Nylon 2,2 – Strength

## Slide 16: Processing Nylon
Injection molding
  Shrinkage (crystallinity)
    .018 in/in
  Dry it first
Extrusion
  Low melt viscosity (process at temp just high enough to melt)
  Be careful of decomposition (especially if not dried)
Fibers
  Drawing
    Crystallization
    Orientation

## Slide 17: Nylon History
Nature of polymer bonding not understood
Carothers
Di-functional monomers
Polymers—1000 units long
  Larger units—molecular still to eliminate water
Control of melting point and length
  Many combinations of polyesters
  Trying polyamides
  Settling on 6,6
Carothers death
  3 weeks after patents
Tremendous success

## Slide 18: Aramids

## Slide 19: Aramids
Amide group
All else is aromatic

## Slide 20: Acetals or Polyoxymethylenes (POM)

## Slide 21: Acetals or Polyoxymethylenes (POM)
(
)n

## Slide 22: Acetal Family Characteristics (compared to nylon 6/6)
Mechanical—do not embrittle, good impact strength
Moisture—very little (shower heads)
Chemical resistance—very high, resists stains, sensitive to strong acids and bases
Weathering—fair
Thermal—200o F
Electrical—good
Machining—like cutting brass
Adhesion—not very good (epoxy glues needed)

## Slide 23: Processing Acetals
Do not heat above 440o F
Melt viscosity is not too dependant on temperature
Do not leave in barrel overnight
  Startup heating

## Slide 24: Acetal Copolymer
(
(
n
Prevents unzipping

## Slide 25: Thermoplastic Polyesters (PET/PBT)
Third largest polymer in production
(behind PE and PP)

## Slide 26: Thermoplastic Polyester General Family Characteristics
PET (compared to nylon 6/6)
  Higher mechanical stiffness
  Strength by orienting chains not by H-bonding
  Get 50% crystallinity
    Forced by mechanical stretching
    Clear because crystalline structures are <500nm
PBT
  Crystallizes rapidly
  Processes faster
  Lower overall properties

## Slide 27: Thermoplastic Polyesters (PET/PBT)
(
)n
PET/PBT
m = 2 or 4
[
]m

## Slide 28: Processing PET
Shape it (film, tape, fiber, extrude, etc)
  Amorphous structure
Reheat and stretch in strength direction(s)
Cool to below Tg

## Slide 29: Specific TP Polyester Types
Dacron fiber—mix with cotton or wool-gives permanent creases
Kodel – photo film
Mylar—transparencies, tapes, balloons
PETG—large glycol modified, amorphous

## Slide 30: Polycarbonate

## Slide 31: Polycarbonate
(
)n

## Slide 32: History
Poor solvent resistance (DuPont)
GE-Lexan (now Sabic)
Properties
  Polar
  Stiffness of backbone
  Long repeat unit
  Bis-Phenol-A (BPA) problems
  Stress-crack problems

## Slide 33: Properties
Solvent sensitivity—poor but nice for joining
Clear—except for UV yellowing, slight crystallinity
Hard
Ductile—nailed, sawed, drawn, punched, sheared, drilled
Tough—helmets, light covers, windows, roadside signs, bullet proof shields
Dimensional stability—low creep
Electrical resistance—good but not fantastic
Machining—good

## Slide 34: Acrylics (PMMA and PAN)

## Slide 35: Acrylics (PMMA also PAN)
(
)n
(
)n

## Slide 36: Properties
Weathering—best
  Color (transparency)—20 years w/ <10% change
Color compatibility (pigments, dyes)
Mechanical properties—average except for impact (brittle) and flex (carpets)
Chemical—chlorinated solvents attack it, acetone gives it cracks
Electrical—good (especially arc resistance)

## Slide 37: Uses
Signs
Counter tops—Corian
Decorative pieces
Floor waxes
Paint, fingernail polishes
Contact lenses, glasses
Fibers (PAN)
  Carbon fibers

## Slide 38: Processing
Casting (sheets)—syrup
Injection molding—good
Thermoforming—ok but brittle
Machining—similar to wood

## Slide 39: Fluoropolymers

## Slide 40: Fluoropolymers (PTFE)
)n
)n
(
(

## Slide 41: History of Discovery
Chambers plant
  Making Freon
  Gas cylinder
Problems with sticking
Problems with processing
Goretex®

## Slide 42: Properties
Most are strengthened by the tight bond between the Fluorine and the Carbon atoms
  Slippery (anti-stick surfaces)
  Chemical inertness
  High temperature melting
  Non-flammable
  High electrical resistance
  Very dense—2.13-2.2 (high melt viscosity)

## Slide 43: Fluoropolymers
―C―C―
F
F
F
OCF3
)n
(
―C―C―
F
F
F
CF3
)n
(
a) Perfluoroalkoxy (Teflon-PFA)
b) Polyhexafluoropropylene (PHFP)
c) Fluorinated ethylene propylene (FEP)
―C―C―
F
F
F
CF3
)m
(
―C―C―
F
F
F
F
)n
(

## Slide 44: Fluoropolymers
―C―C―
Cl
H
Cl
H
)n
(
―C―C―
H
F
H
F
)n
(
b) Polyvinylidenechloride (PVCl2 ― Saran wrap)
a) Polyvinylidenefluoride (PVDF or PVF2 ― Tedlar)
―C―C―
F
F
F
SO3Na
)n
(
c) Nafion

## Slide 45: Fluroroelastomers
Viton (copolymers)
―C―C―
F
F
F
CF3
(PHFP)
―C―C―
H
F
H
F
(PVDF)
+
+
―C―C―
F
F
F
F
PTFE
―
―
―

## Slide 46: Uses
O-rings
Non-stick surfaces
Insulation-electrical
Lubricant
Coatings
Gears

## Slide 47: Processing
PTFE not processible by extrusion or injection molding
  Sintering
    Put in approx shape and heat to about 650oF (melt = 664°F)
    Similar to processing powdered metals
    Fusion of particles
  Ram extrusion
    Compaction
    Rods and tubes
  Calendaring
Very poor adhesion

## Slide 48: High Performance Thermoplastics

## Slide 49: Polyphenylenes (PPE, PPO, PPS)
PPO

## Slide 50: Polyphenylene Oxide (PPO) Properties
Thermal stability—excellent (650o F)
High HDT = 375o F
Good cold properties (-275o F)
Low water absorption
Low heat expansion
Good solvent resistance, but can be solvent welded
O
O
CH3
CH3
CH3
CH3
(
)n

## Slide 51: PPO uses
Used to replace stainless steel for surgical equipment
Replace thermosets
Pump housings
Valve components
Video terminal housings

## Slide 52: Polyaryletherketones (PEEK, PEK, and Others)
Inside of hip replacement
is PEK
+

## Slide 53: Polyaryletherketones (PEEK, PEK, and Others)
Ether Linkage
Ketone Linkage

## Slide 54: Polysulfones (PSU and PES)

## Slide 55: Polysulfones (PSU and PES)

## Slide 56: PSU and PES Properties
Resistant to oils
Heat stability (300o F)
Creep resistance
SO2 group adds stiffness
More dimensionally stable than PPO
Toughness—good

## Slide 57: PSU and PES Uses
Hot water pipes
Coffee pots
Dishwasher components
Automobile applications near engines
Compete with thermosets, but can be injection molded

## Slide 58: Thermoplastic Polyimides (PI and PAI)

## Slide 59: Thermoplastic Polyimides (PI and PAI)
(
)n
)n
(
Imide

## Slide 60: Thermoplastic PI and PAI Properties
Very stiff
Highest thermal stability
PI cannot be melted or melt processed
PAI can be (Torlon)
PI is sintered (Vespel)
PI film is cast as monomers and heated to polymerize (Kapton)

## Slide 61: Thermoplastic PI and PAI Uses
PI is used in circuit boards (Kapton film)
High temperature parts (Vespel – sintered)
Low friction bearings, sliding parts, gears
  Filled Vespel (Mo, carbides)

## Slide 62
Flammability of aircraft seats with PBI foam
PBI foam
Conventional foam

## Slide 63: Cellulosics

## Slide 64: Cellulosics
Nitrocellulose
  Gun cotton
  Explosive billiard balls (past product)
  Movie films
Cellulose nitrate
  Lacquers and plastics

## Slide 65: Types of Cellulosics
Rayon
  Viscose process
Cellophane
Methyl cellulose
  Filler
  Edible (hydroxypropyl methyl cellulose)

## Slide 66: Thank You
Brent Strong