## Slide 1: Thermoset Materials
MFG 355

## Slide 2: Introduction
Thermoplastics vs Thermosets
  Thermal properties
  Strength
  Uses
  Processing

## Slide 3: Resin Rules
Resin Rule: Thermoset resins depend upon two chemical reactions for their properties:
  Polymerization
  Crosslinking (curing)

## Slide 4: Thermal Effects During Reactions
Molecular collisions are required for reactions
Heat increases molecular movement and collisions
The rate (speed) of chemical reactions increases as the temperature is increased
  Arrhenius equation: exponential relationship between rate and temperature
  Rate roughly doubles for each 10°C rise
Some reactions create heat (exotherm)

## Slide 5
Viscosity
Time/Temperature
Liquid-Solid Line
Solids
Liquids
Thermoset
thinning due to
temperature
Thermoset
crosslinking
Thermoset
combination
(What is seen)
Gel Point
Thermoplastic
Viscosity curves for typical
thermoplastics and thermosets
Processing Window

## Slide 6: General Properties of Thermosets
Crosslinking (always)
Strength (good)
Flexibility (poor)
Thermal (good)
Creep (low)
Ability to wet-out reinforcements (good)
Ability to cure at room temperature (some)

## Slide 7: Formaldehyde Resins

## Slide 8: Resin Rules
Resin Rule: For some polymers both polymerizing and crosslinking reactions can occur simultaneously.
  The reactions can often be stopped before completion to allow easier handling and forming of the polymer
    When this is done, the intermediate material is called the B-stage and the processing is called B-staging.

## Slide 9
+
3-D Phenolic
Crosslinked Network
Formaldehyde
Phenol
Loss of
Water
*
*
*
(* = Active site)
Phenolic polymerization and crosslinking
O
H
H
H
C
O

## Slide 10: Phenolics − Processing
Problem | Solution
Toxic monomer (formaldehyde) | B-staging to novolac (solid, 2-step with hexa) or resole (liquid,1-step)
Condensation of water | Slow cures and venting of mold (compression molding)
High shrinkage | Fillers (minerals, sawdust, wood flour, ground nut shells, etc.)
Brittleness | Fillers (selected) and thickness of parts
Inconsistent color | Black pigment

## Slide 11: Phenolics
Aromatic content determines most of the applications of phenolics
  Very low flammability and low smoke
  Very stiff and hard
  Very low heat transfer
  High thermal stability
  Good electrical properties
  Excellent adhesion
  Resistance to chlorinated solvents
  Moderately low price (10-15% above polyesters)

## Slide 12: Phenolics
Applications
  Interiors of public transportation
  Glue for laminates (such as plywood)
  Electrical switches and other equipment
  Molded parts in moderately hot environments (such as near the motor of an automobile)
  Billiard balls
  Conversion to epoxy or vinyl ester resins
  Rocket exit nozzles and carbon-carbon composites (ablation)

## Slide 13
10
20
30
40
Vinyl Ester
Epoxy
FR Polyester
Phenolic
(ASTM E-162 for thermoset
composites)
Vinyl Ester
Epoxy
FR Polyester
Phenolic
(ASTM E-662 for thermoset
composites)
100
Specific Optical Density
Flame Spread Index
200
300
400
500
600
Phenolic flammability

## Slide 14
700-
600-
500-
400-
300-
200-
100-
0 2 4 6 8 10 12 14 16 18 20 22
NBS Smoke Chamber (Smoldering)
Epoxy
Polyester
Phenolic
Optical
Density
Time (min)

## Slide 15
Rocket Exit Throat
Exit Nozzle
(Ablative
Material)
10 oF
500 oF
4000 oF
Rocket
Motor
Rocket
Propellant
Nose
Cone
Rocket exit nozzle with phenolic as the ablative material

## Slide 16: Carbon-Carbon
Brake Pads

## Slide 17: Carbon-Carbon Composites
Carbon matrix and carbon fibers
Carbon matrix is made from phenolic resins that have been repeatedly charred and infused (infiltrated) with new resin
  Very long process (up to 6 months for a part)
  Very costly
Extremely high thermal stability
  Needs flammability coating (ceramic) at very high temperatures

## Slide 18
Cured Carbon/Resin Part
Pyrolize
1000-1500oC
Impregnation by
Gas or Liquid
Heat Treatment
2000-2800oC
Carbon/Carbon
Composite
Polymer or Pitch
Binder
Carbon Fiber
Production flow chart for carbon-carbon composites

## Slide 19
106-
105-
104-
103-
102-
10-
1-
0 1000 2000 3000 4000
-18 538 1093 1650 2204
Temperature
oF
oC
Exposure
Time
(sec)
Epoxy Composites
Polyimides
Advanced
Metalics
Carbon-Carbon
Experimental
Ablative Materials
(such as phenolics)
Retention of properties of various composites with time and temperature

## Slide 20: Amino Plastics
Amine
Plus
Formaldehyde

## Slide 21: Amine plastics – clear adhesive
Chipboard

## Slide 22: Melamines
Melamine
Three
active
sites
Formaldehyde
Plus
Melamine
Formaldehyde

## Slide 23: Melamines

## Slide 24: Unsaturated Polyesters

## Slide 25: Resin Rules
Resin Rule: Polymerization of unsaturated polyesters occurs by the condensation method.
  Polyester = a polymer in which ester groups are the repeating units
  Unsaturated = contains carbon-carbon double bonds after polymerization (but before crosslinking)
  Polyesters are made from two types of monomers:
    Di-acids
    Glycols (di-alcohols)

## Slide 26: Polyester polymerization
Monomers
Glycols G
(di-alcohols)
Acids A
(di-acids)
G
G
G
G
A
A
A
A
A
Polyester polymer

## Slide 27: Polyester polymerizationn
One end of the di-acid (the OH group) reacts with one end of the glycol (the H group) to form water (H−OH)
  The water separates from the polymer and condenses out as a liquid
    These type of polymerization reactions are called condensation reactions
  A new bond is formed where the water left

## Slide 28
HO―G―OH
Glycol
O
H
C
A
C
O
H
O
O
Di-acid
Step 1: Monomers react
+
Step 2: New molecule reacts with new monomers
O
O
HO―G―O―C―A―C―OH
+
HO―G―OH
Glycol
O
H
C
A
C
O
H
O
O
Di-acid
+
Ester
Ester
Ester
O
O
O
O
HO―C―A―C―O―G―O―C―A―C―O―G―OH
Polymerization of a typical polyester
HO―G―O―C―A―C―OH
O
O
Ester
New bond
+ H2O
+ 2 H2O

## Slide 29: Resin Rules
Resin Rule: The types of di-acids and glycols and their percentages determine the properties of the unsaturated polyester.
  The amount of unsaturated di-acid controls the amount of crosslinking (crosslink density)
  Several types of di-acids and glycols can be mixed to form polymers with specific properties
    Aromatic/aliphatic, halogenated, polar, etc.

## Slide 30
C C
―
―
│
COOH
│
│
│
HOOC
H
H
C C
―
―
COOH
HOOC
│
│
│
│
H
H
C C
―
―
H
H
│
│
│
│
C=O
O=C
O
Structure
Name
Comments
Fumaric acid
Maleic acid
Maleic anhydride
Trans isomer,
highly reactive,
crosslinkable
Cis isomer,
converts to fumaric acid,
crosslinkable
Readily converts to
maleic acid and
fumaric acid
in presence of water,
crosslinkable
Unsaturated di-acid monomers

## Slide 31
―C―OH
―C―OH
Structure
―C
―C
O
│
│
│
│
O
O
│
│
│
│
O
O
Name
Orthophthalic acid (ortho)
Orthophthalic anhydride
Comments
Low cost,
styrene compatible
Converts to ortho
Saturated di-acid monomers
―C―OH
―C―OH
│
│
│
│
O
O
Isophthalic acid (iso)
Strength, thermal,
water/chemical resistance

## Slide 32
Structure
―C―OH
HO―C―
HO―C―CH2―CH2―CH2―CH2―C―OH
│
│
│
│
│
│
│
│
O
O
O
O
―C
―C
O
│
│
│
│
O
O
│
│
Br
Br
Br
Br
Name
Terephthalic acid (tere)
Adipic acid
Tetrabromophthalic
anhydride
Comments
Thermal stability
Tough,
weatherable
Flame retardance
Cl―CH2―CH―CH―C―OH
Cl―CH2―CH―CH―C―OH
│
│
O
│
│
O
C
Cl
Cl
Chlorendic acid
Flame retardance,
chemical resistance
Saturated di-acids

## Slide 33
Structure
Name
Comments
Glycol monomers
HO―CH2―CH2―OH
HO―CH2―CH―OH
│
CH3
HO―CH2―CH2―O―CH2―CH2―OH
HO―CH2―C―CH2―OH
│
CH3
CH3
│
―C―
│
CH3
CH3
│
HO―
―OH
Ethylene glycol
Propylene glycol
Diethylene glycol
Neopentyl glycol
Bisphenol A
Low cost
Styrene compatibility
Flexibility, toughness
Weathering,
water/chemical resistance
Strength, toughness,
water/chemical
resistance

## Slide 34
Polyesters − specific molecules
Crosslinking occurs at the carbon-carbon double bonds
the number of which can be increased during polymerization
Acid
Acid
Acid
Acid
Acid
Acid
Acid
Glycol
Glycol
Glycol
Glycol
Glycol

## Slide 35: Resin Rules
Resin Rules: Unsaturated polyesters cure by a chain reaction mechanism that is started by an initiator molecule reacting with a carbon-carbon double bond.

## Slide 36: Crosslinking Reaction
Called addition or free radical crosslinking reaction
Proceeds as a chain reaction
  Once started, it will keep going unless specifically terminated
  Doesn’t need more initiator
  Makes its own reactive sites

## Slide 37: Initiators
Initiators are sometimes called catalysts.
The most common initiators are peroxides.
The peroxides are effective initiators because they split into free radicals which react easily with the double bonds.
Free radicals have unshared electrons.
I–I  I + I
Peroxide Initiator
Free radical
Reaction can be heat or chemical induced

## Slide 38: Polyesters − crosslinking (curing)
C
C
C
C
Carbon-carbon double bond
(Unsaturated portion)
Polyesters must have unsaturated portions to crosslink

## Slide 39: Polyesters − crosslinking (curing)
C
C
C
C
I
Initiator
●
Initiation

## Slide 40: Polyesters − crosslinking (curing)
C
C
C
C
I
●
●
●
Reacting with the carbon-carbon double bond

## Slide 41: Polyesters − crosslinking (curing)
C
C
C
C
I
●
Bond (2 electrons)
Unshared electron or
free radical (reacts readily)
Formation of a bond and a new free radical
To react and form a crosslink, the free radical on the polymer needs to encounter (collide with) a double bond on another polymer
The polymers are long and entangled (highly viscous), thus they don’t move very quickly
The chances of lining up just right are not good

## Slide 42: Polyesters − Solution to the problem
Dissolve (dilute) the polymer in a solvent
  Ideally, the solvent will react during crosslinking
    These types of solvents are called “reactive solvents” or “reactive diluents” or “co-reactants”
Styrene is the most common diluent
Added benefit: The solvent will also reduce the viscosity so that the polymer will wet the fibers more easily if used in a composite
or

## Slide 43: Polyesters − crosslinking (curing)
C
C
C
C
I
●
Bond (2 electrons)
Styrene molecule
is attacked at
double bond site
C
C
C
C
C
C
C
C

## Slide 44: Polyesters − crosslinking (curing)
C
C
C
C
I
Bond (2 electrons)
Formation of a new bond
and a new free radical
C
C
C
C
C
C
C
C
●
Can link to another unsaturation site
(usually on another styrene molecule or another polymer)

## Slide 45: Polyester − forming the crosslink
C
C
C
C
I
Styrene
C
C
C
C
New free radical
●
New bonds
(crosslink)
The new free radical is available to react with another styrene

## Slide 46: Continuing/Terminating
Once started, the free radical-based reactions will continue until one of the following conditions is met:
  Reactive diluent (styrene) is not available
  Stops encountering other polymers’ double bonds
    Post-curing can improve crosslinking
  The free radical site meets another free radical site on another polymer
  The free radical site meets another initiator free radical
    Danger of adding too much initiator
  The free radical reacts with a terminator molecule
    Ozone is commonly used

## Slide 47: Inhibitors
Inhibitors are added to increase storage time, usually by the resin manufacturer
  Inhibitors typically absorb free radicals
  Inhibitors protect the polymer during storage because sunlight, heat, contaminants, etc. can start the curing reaction
  Molders must add sufficient initiator to overcome the inhibitors and to cause the crosslinking to occur

## Slide 48: Promotors (accelerators)
Added to the polymer to make the initiator work more efficiently or at a lower temperature
  Each type of peroxide has a temperature at which it will break apart into free radicals
  These temperatures are usually above room temperature
  For room temperature curing, a chemical method for breaking apart peroxides is needed
The most common promoters (accelerators) are cobalt compounds and analines (DMA)
Never add a promoter directly into an initiator

## Slide 49: Additives
Additives are components (usually minor) that have various functions that are not related to the curing reaction
The most common types of additives are:
  Fillers (to lower cost and/or give stiffness)
  Thixotropes (to control viscosity)
  Pigments
  Fire retardants
  Surfactants (to promote surface wetting)
  UV inhibitors/Anti-oxidants

## Slide 50
180
240
280
0
5
10
15
Time, min
Temperature, °F
oC
82
115
138
Exotherm temperature
Gelation point
Gel time
Time to exotherm
The cure reaction is followed by
measuring gel time and exotherm

## Slide 51
Thickness, inches
Peak exotherm, °F
│
│
│
│
│
1.25
1.5
1.75
2.00
2.25
2.50
―
―
―
260
280
300
320
340
―
Heat buildup as a function of thickness of the curing part

## Slide 52: Epoxies

## Slide 53: Epoxies
Second most widely used family of thermosets (after polyesters)
Large portion of uses are non-reinforced (adhesives, paints, etc.)
Circuit boards are the largest reinforced application (low conductivity, low volatiles)
Advanced composites use epoxies because of:
  Thermal stability
  Adhesion
  Mechanical properties

## Slide 54
Epoxy and glycidyl groups
H―C―C―R
│
│
H
H
O
H―C―C―C―R
│
│
H
H
O
│
H
│
H
a) Epoxy group
b) Glycidyl group
Generalized organic group

## Slide 55
C
C
Epoxy ring (or glycidyl group)
O
C
C
O
(
)n
Polymer portion
Number of repeat units
Generalized epoxy polymer

## Slide 56
―C―
│
CH3
CH3
│
HO―
―OH
Bisphenol A
Cl―CH2―CH―CH2
O
+
Epichlorohydrin
A common epoxy synthesis reaction
―C―
│
CH3
CH3
│
―OCH2CHCH2O―
―O―
CH2―CH―CH2
O
O
CH2―CH―CH2
+ nHCl
Diglycidyl Ether of Bisphenol A (DGEBPA)
Glycidyl
(
)n
n reactions
│
OH

## Slide 57: Resin Rules
Resin Rule: The number of epoxy groups determines the amount of crosslinking.
  Epoxy groups are at the end of a chain
  Chains containing epoxy groups can be repeated so that a molecule can have several epoxy groups
  High crosslinking gives thermal stability but requires high curing temperatures

## Slide 58
O
CH2―CH―CH2―O―
O―CH2―CH―CH2
O
│
―O―CH2―CH―CH2
O
Tri-functional epoxy
High temp applications OK but requires high temp cure and post cure.
Multiple epoxy groups increases crosslinking

## Slide 59
Tetraglycidylmethylenedianiline (TGMDA)
Tetraglycidyldiaminodiphenylmethane (TGDDM)
CH2―CH2―CH―CH2
O
CH2―CH2―CH―CH2
O
H2C―CH―CH2―CH2
O
H2C―CH―CH2―CH2
O
Tetra-functional epoxy
―CH2―C―CH2―
│
CH3
CH3
│
N―
―N
Standard of high performance resins for 40 years
Exotherm can be very high (depending on curing agent).
-Control: thickness, heat-up rate, number of temperature holds.
Thermal stability, high degree of crosslinking

## Slide 60
―CH2―
―CH2―
(
)n
│
│
CH2
O
│
CH
│
CH2
O
│
│
CH2
O
│
CH
│
CH2
O
│
│
CH2
O
│
CH
│
CH2
O
Novolac-based epoxy resin (Epoxydized phenolic resin)
High density of crosslink sites can give high Tg. High temp cure is usual.
The central chain is a repeat unit (n repeats)

## Slide 61
―C―
│
CH3
CH3
│
H2C― CH―O―
―O―
CH2―CH―CH2
O
O
Br
Br
Br
Br
A flame retardant epoxy (TBBA)
Low flame spread but high smoke and choking fumes.

## Slide 62: Resin Rules
Resin Rule: Epoxies use hardeners instead of initiators for curing.
  Hardeners open the epoxy ring and link to the main epoxy chain
  Hardeners have active groups at both ends so that they can crosslink two molecules together

## Slide 63: Curing
C
C
Epoxy ring
O
C
O
(
)n
Epoxy ring
N
N
H
H
H
H
N
N
H
H
H
H
C
Hardener molecules have two
reactive ends, so they can each
react with two epoxy molecules.

## Slide 64
Epoxy Crosslink Mechanism
C
C
H
H
Hardener
Epoxy
The other ends can also react (usually with other molecules).
Cured Polymer

## Slide 65: Resin Rules
Resin Rule: Many different hardeners are available to cure epoxies.
  Very active ends on the hardener molecule allows crosslinking at lower temperatures
  Hydrogens attached to highly electronegative atoms are very active
  Nearby aromatic groups decrease activity
  Nearby large groups of atoms hinder access and therefore decrease activity

## Slide 66: Effects of various hardeners
Hardeners | Advantages | Disadvantages
Aliphatic amines | Convenience, low cost, room temp cure, low viscosity | Skin irritant, critical mix ratios, blushes
Aromatic amines | Moderate heat resistance, chemical resistance | Solids at room temp, long and elevated cures
Polyamides | Room temp cure, flexibility, toughness, low toxicity | High cost, high viscosity, low HDT
Amidoamines | Toughness | Poor HDT
Dicyandiamide | Good HDT, good electrical | Long, elevated cures
Anhydrides | Heat and chem resistance | Long, elevated cures
Polysulfide | Moisture insensitive, quick set | Odor, poor HDT
Catalytic | Long pot life, high HDT | Long, elevated cures, poor moisture
Melamine/form. | Hardness, flexibility | Elevated temp cure
Urea/form. | Adhesion, stability, color | Elevated temp cure
Phenol/form. | HDT, chem resistance, hardness | Solid, weatherability

## Slide 67: Curing Profile
Vacuum
355±10
Temperature (°F)
Time
0
100
200
300
400
Begin heat after full pressurization of autoclave
130
120 minutes
1-5°F/minute (critical for precipitate)
Autoclave

## Slide 68: Curing Profile
Why 2-stage?
  To minimize exotherm
  To allow time for gas escape before hardening completely
  Not required in parts less than 0.5 inches thick
Danger of curing too quickly (ramp rate, etc)
  Exotherm
Why such long time at highest temperature?
  Molecular mobility gives full cure (crosslinking)

## Slide 69: Epoxy and Polyester Comparison
Comparisons | Polyester | Epoxy
Active site | C=C | 
Crosslinking reaction | Addition/free radical | Ring opening
Crosslinking agent | Initiator (peroxide) | Hardener
Amount of x-link agent | 1-2% of resin | 1:1 with resin
Solvent/viscosity | Styrene (active)/low | Infrequent/high
Volatiles | High | Low
Inhibitors, accelerators | Frequent | Infrequent
Reactant toxicity | Low | Moderate
Cure conditions | Room temp or heated | Heated (some room)
Shrinkage | High | Low
Post cure | Rare | Common

## Slide 70: Polyester and Epoxy − Properties
Property | Polyester | Epoxy
Adhesion | Good | Excellent
Shear strength | Good | Excellent
Fatigue resistance | Moderate | Excellent
Strength/stiffness | Good | Excellent
Creep resistance | Moderate | Moderate to good
Toughness | Poor | Poor to good
Thermal stability | Moderate | Good
Electrical resistance | Moderate | Excellent
Water absorption resist | Poor to moderate | Moderate
Solvent resistance | Poor to moderate | Good
UV resistance | Poor to moderate | Poor to moderate
Flammability resistance | Poor to moderate | Poor to moderate
Smoke | Moderately dense | Moderately dense
Cost | Low | Moderate

## Slide 71: Vinyl Esters

## Slide 72: Resin Rules
Resin Rule: Curing properties of a polymer can be modified by appropriate chemical substitution.

## Slide 73: Vinyl Esters
Epoxy resins that have been modified so that they can be cured like a polyester
  The modification is usually a reaction with an acrylic (acrylic modified epoxy)
  The modification must substitute a carbon-carbon double bond for the epoxy ring
The name, vinyl ester, comes from old chemistry

## Slide 74
C
C
C
C
(
)n
Unsaturated end group
Unsaturated end group
Often an epoxy backbone
Typical vinyl ester polymer

## Slide 75
Epoxy (typical)
―O―
O
CH2―CH―CH2
…
CH2―CH―C―O―H
―
│
│
O
Acrylic acid
+
Attack and bond
Broken bond
Bonding
―O―
O–H
CH2―CH―CH2
…
CH2―CH―C―O―
―
│
│
O
Synthesis of a vinyl ester from an epoxy
Vinyl ester (typical)
Note: The carbon at which the
molecules link is bolded

## Slide 76
Epoxy Novolac Vinyl Ester Resin
Bisphenol-A Epichlorohydrin-based vinyl ester
(
)n
Typical Vinyl Esters

## Slide 77: Vinyl esters − Properties
Almost all properties of vinyl esters (and cost) are intermediate between polyesters and epoxies
Some of the most important properties include:
  Water and chemical resistance
  Electrical stability
  Thermal stability
  Toughness
  Low volatiles during manufacture
  Low shrinkage

## Slide 78
―
―
―
―
―
―
0
2
1
3
4
5
6
Weight gain (%)
│
│
│
│
│
0
50
100
150
200
250
Exposure time (hours)
□
□
□
□
□
Vinyl ester resin (fewer polar groups)
●
●
●
●
●
Polyester resin
Weight gain in water of polyester and vinyl ester resins

## Slide 79: Resin Rules
Resin Rule: Aromatic-like properties can be obtained from inclusion of groups other than benzene rings.
  The object of such substitution is usually for thermal stability.
  These resins are usually very difficult to process.
  The resins usually also contain many benzene rings to further enhance aromaticity.

## Slide 80: Polyimides

## Slide 81: Resin Rules
Resin Rule: Aromatic-like properties can be obtained from inclusion of groups other than benzene rings.
  The object of such substitution is usually for thermal stability.
  These resins are usually very difficult to process.
  The resins usually also contain many benzene rings to further enhance aromaticity.

## Slide 82
R―N
C―C
C―C
│
│
│
│
│
O
O
R
R
R = other atoms or groups
a) Imide group
Imide group and its inclusion in a polymer
C
C
│
│
│
│
O
O
N―R―
)n
C
C
│
│
│
│
O
O
―N
(
b) Imide group in polymer

## Slide 83
Bismaleimide (BMI)
Crosslink sites
Crosslinks using the unsaturated polyester reaction
Has very good thermal stability compared to epoxies

## Slide 84
―
―
―
―
―
2
4
6
8
10
Weight loss (%)
│
│
│
│
│
100
0
0
200
300
400
500
Hours
Thermal stability of a PMR-15 composite
800°F (427°C)
700°F (371°C)
600°F (315°C)

## Slide 85
Crack
Microspheres filled with DCPD
Polymer
•
•
•
•
•
•
•
•
•
•
•
•
Catalyst
•
•
•
•
•
•
•
•
•
•
•
•
Propagation
of crack
through
microsphere
•
•
•
•
•
•
•
•
•
•
•
•
•
•
•
Cracks filled
with DCPD
which cures
when it
encounters
catalyst in the
body of the polymer
Mechanism of self-healing of a polymer
•
•
•

## Slide 86: Thank You
Thermosets