## Slide 1: Elastomers
MFG 355

## Slide 2: Elastomeric Materials
Highly amorphous
Highly random orientation
High elongation

## Slide 3: Elastomeric Materials
Chart: Stress
Metals
Conventional Plastics
Elastomers
Stress
Strain

## Slide 4: Elastomeric Materials
No Stress
Stressed
In tension
Recovery
from Entropy

## Slide 5: Elastomeric Materials
No Stress
Stressed
In tension
Crosslinks
Recovery
from Entropy
and Crosslinks
Crosslinks
(stretched)

## Slide 6: Aliphatic Thermoset Elastomers
These are the most common elastomers
These have a double bond after polymerization has occurred
These are noncrystalline
These are highly flexible

## Slide 7: Natural Rubber
Hevea Rubber
(cis-polyisoprenene)
Gutta percha or Balatta
(trans-polyisoprene)

## Slide 8: Natural Rubber
Raw material extracted from trees

## Slide 9: Natural Rubber
Material is processed

## Slide 10: Natural Rubber
Latex is then dried, sorted and smoked

## Slide 11: Natural Rubber
The difficulties with natural rubber
  Strength
  Availability
  Bacterial breakdown
  Creep

## Slide 12: Natural Rubber
Creep
  Solved by Goodyear in the 1800's
  Discovered that the polymer could be crosslinked (cured or vulcanized) by heating with sulphur
Sulphur attacks this double bond
- As many as 2-8 sulphur atoms might
be in the bridge between molecules

## Slide 13: Vulcanization

## Slide 14: Synthetic Polyisoprene or Isoprene Rubber
Need
  Supply of natural rubber disrupted during WWI and WWII
  Used in tires for bicycles and early cars
  Used the Ziegler-Natta catalyst system to improve properties
    The trans- or cis- nature of the rubber could be controlled up to 90% in either direction

## Slide 15: Butadiene Rubber (BR)
How is this polymer different from natural rubber?

## Slide 16: Butadiene Rubber (BR)
No cis or trans isomers
Lower mechanical strength because of no of pendant methyl group but also more flexibility
Lower cost (all synthetic from cheap monomer)
Improvement of low-temp flexibility
Compatibility with other polymer materials

## Slide 17: Styrene Butadiene Rubber (SBR)

## Slide 18: Butyl rubber
Also known as polyisobutylene
Butyl bullets for less lethal control

## Slide 19: Oil-Resistant Elastomers
NBR—Nitrile Butadiene Rubber
  Copolymerization of butadiene and acrylonitrile
  More expensive than SBR or BR
CR—Chloroprene rubber (neoprene)
  Thermal stability
  Non-flammable

## Slide 20: Ethylene-Propylene-Butadiene Monomer (EPDM)
C
C
H
C
C
C
H
H
H
H
H
H
H
H
H
[
[
[
E monomer
P monomer
Butadiene monomer

## Slide 21: Thermoplastic Elastomers (EPM and EPDM)
Many of the properties of thermoset elastomers
  Resiliency
  Elasticity
More easily processed
  Injection molding, extrusion and other standard thermoplastic processes
  Highly compatible with polyolefins
  EPDM is crosslinked very lightly and may not be capable of being melted

## Slide 22: Thermoplastic Olefin Elastomers (TPO)
Poor compatibility with other rubbers
Melt processible

## Slide 23: Flouroelastomers
Vinylidene fluoride monomer
Tetrafluoroethylene monomer
+
Copolymer = Viton®

## Slide 24: Flouroelastomers
Many of the desirable properties of flouropolymers
  Low solvent effects
    Excellent for chemical and petroleum handling applications
  High thermal stability
    Good for gaskets and seals

## Slide 25: Silicones
(
)n
(
)n
i

## Slide 26: Silicones

## Slide 27: TPE – Polyurethanes

## Slide 28: Polyurethanes
Plus
Polyols
Diisocyanates

## Slide 29
HO
OH
C=N
O
=
N=C
O
=
+
HO
O
C
O
N=C
O
=
=
N
H
Urethane
linkage
Polyol
Di-isocyanate
Urethane linkage formation
Note: This is a rearrangement reaction (like condensation but no condensate)

## Slide 30: TPU Chemistry: A+B
A: Hard Segment
B: Soft Segment
Long chain polyol
Diisocyanate (aromatic or aliphatic)
Short chain polyol (chain extender)
Chain Extender
Isocyanate
Polyol

## Slide 31: Hard Segment Properties
Diisocyanate + Chain Extender
  Polymer Strength
  Crystallinity
  Melting Temperature
  Modulus (Stiffness)
  Hardness
  Heat Resistance
  Biocompatibility
  Aromatic or Aliphatic Isocyanates

## Slide 32: Hard Segment Diisocyanates and Chain Extenders
Aromatic Isocyanates
MDI (Methylenediphenylisocyanate)
TODI (Tolidine Diisocyanate)
PPDI (Paraphenylenediisocyanate)
NDI (Napthalenediisocyanate)
Aliphatic Isocyanates
HMDI (Methylenediphenylisocyanate)
TMXDI (ETA-Tetramethylxylenediisocyanate)
CHDI (Cyclohexanediisocyanate)
HDI (Hexamethylenediisocyanate)
Chain Extenders
BDO (1,4 Butanediol) – Di-functional
HQEE (Hydroquinonedi-B-Hydroxyethylether) – Di-functional
TMP (Trimethylolpropane) – Tri-functional
DG (Di-Ethylene glycol)
Many others

## Slide 33: Soft Segment Properties
Long Chain Diol
  Polymer Elasticity
  Resilience
  Solvent Resistance (Solubility Parameter)
  Biocompatibility
  Low Temperature Properties
  Glass Transition Temperature
  Phase Separation
  Mechanism to introduce alternative chemistries to the polymer backbone for compatibility and reactivity

## Slide 34: Soft Segment Polyols
Ester Based
  PBA (Polyester Butylene Adipate)
  PEA (Polyester Ethylene Adipate)
  Polycaprolactone Ester
  Polycarbonate Ester
Ether Based
  PTMO (polytetramethyleneoxide)
  PSX (polydimethylsiloxane) + PTMO
  PTMEG (polytetramethyleneglycol)
  PPO (Polypropylene oxide)
  PEG (Polyoxyethylene glycols)
  Perfluorinated Polyethers
Various Modifications
Various Molecular Weight/Distribution

## Slide 35: Thermoplastic Polyurethane (TPU)

## Slide 37: Elastomer Processing
Compounding
  Banbury mixer

## Slide 38: Elastomer Processing
Preforming
Molding
Dipping

## Slide 39: Impact Toughness Guide
Resin | Izod (ft-lb) | Reasoning
Polyurethane (x-link) | 25 | High elongation and strength
Polycarbonate | 16 | High strength
SMC | 7 | Reinforced and toughened
ABS | 6 | Toughened with rubber
HDPE | 3 | High elongation, flexible
Acetal | 2 | Can be toughened
Nylon 6/6 | 2 | Can be toughened
PET | 1 | Can be alloyed
PP | 1 | Some crystallinity
LDPE | 1 | Low strength
Polystyrene | 0.3 | Pendent group
Acrylic | 0.3 | Short link, large pendent group
Phenolic, w/fiberglass | 0.3 | Crosslinked
Epoxy, unreinforced | 0.2 | Crosslinked
Crosslinked polyester | 0.2 | Crosslinked
Increasing Toughness

## Slide 40: Thank You