## Slide 1: Extrusion
MFG 355

## Slide 2: Extrusion

## Slide 3: Extrusion System
Cutter/
Winder
Puller
Water Bath
Extruder

## Slide 4: Extruder
Barrel
Motor
Hopper
Feed
Feed throat
Heating zones
Die
Linkage
Thrust bearing

## Slide 5: Extruder

## Slide 6: Drive Motor
Turns the Screw
Provides power for the process

## Slide 7: Thrust Bearing
Prevents the screw from moving backward
Seals off the end of the barrel

## Slide 8: Extruder Screw
Connected to drive linkage
Inside barrel
Squeezes the plastic
Moves the plastic

## Slide 9: Extrusion Screws

## Slide 10: Extrusion Screws

## Slide 11: Extrusion Screws
L/D ratio
  Relates directly to the extruder’s ability to mix
  Typical L/D ratio is 16:1 up to 32:1
    Newer machines tend to have higher ratios
Length (L)
Diameter (D)

## Slide 12: Extrusion Screws

## Slide 13: Extrusion Screws
Pitch Angle

## Slide 14: Extrusion Screws
Zones
Shows gaps between barrel and screw root
Material Flow Direction

## Slide 15: Multi-Screw and Multi-Barrel
Valuable in heat sensitive material processing (PVC)
Increases efficiency in moving material
More positive pumping action

## Slide 16: Multi-Screw and Multi-Barrel
Co-Rotating Screws
Counter-Rotating Screws
Advantages and Disadvantages
Co-Rotating Screws
Counter-Rotating Screws

## Slide 17: Head Zone
The portion of the machine at the end of the barrel
Holds/contains the die

## Slide 18: Head Zone

## Slide 19: Head Zone
Breaker plate
  Screens
  Filters
Adaptor
  Die mount

## Slide 20: Die
The “mold” for the extrusion process

## Slide 21: Die
Input (machine) side
Output side

## Slide 22: Die
Dies are cut to produce a certain profile
Cutout will probably not match the finished product
Die
Part
Part
Die
Die

## Slide 23: Spider Die
Material Flow

## Slide 24: Coat Hanger Dies
Correct flow
  Velocity
  Distribution

## Slide 25: Sheet Extrusion

## Slide 26: Wire Coating Dies

## Slide 27: Wire Coating Dies
Bare Wire
Input
Insulated Wire
Output
Heat Unit
Extruder

## Slide 28: Dimensional Control
Sizing Plates

## Slide 29: Part Dimension Control
Die
Gap/Extrudate swell/Draw down
Sizing plate
Air pressure/Vacuum pressure
Cooling (shrinkage)
Speed of pull
ID
OD
Wall Thickness

## Slide 30: Part Dimension Control
Gap/Extrudate swell/Draw down

## Slide 31: Gap

## Slide 32: Part Dimension Control
Sizing plate
Air pressure
Cooling (shrinkage)

## Slide 33: Cooling Tank

## Slide 34: Pullers
Pullers are in contact with cooled material
Pulling quicker will decrease the cross-sectional area of the extrudate

## Slide 35: Puller and Printing

## Slide 36: Extrusion Plant

## Slide 37: Extrusion Plant

## Slide 38: Film Blowing
Extrude a “tube” upwards through vertical die
Inflate “tube” till it becomes a film
Collect film and process as needed

## Slide 39: Film Blowing

## Slide 40: Film Blowing

## Slide 41: Film Blowing
Extruder
Die/Blower
Assembly
Sizing Basket
Nip Rollers
Windup
Frost Line

## Slide 42: Film Blowing
Film Blowing Systems

## Slide 43: Film Blowing
Extruder and Blower

## Slide 44: Fiber Extrusion
Extrusion through an extruder
Spun and stretched as filaments exit the die
Twisted/wound and/or taken up on a roll

## Slide 45: Fiber Extrusion

## Slide 46: Coating of Paper and Fabric
Extrude a film
System of rollers to apply extruded film to paper/fabric
Windup rollers take up coated paper/fabric

## Slide 47: Extrusion Cast Coating
Extrude (blow) a film
Feed film into a machine that has other films that are pressed together (heated)

## Slide 48: Post Extrusion Forming
Corrugated pipe
Perforated pipe
Bell ended pipe

## Slide 49: Coextrusion
Join two streams of molten plastic into one
Separate extruder for each stream (typically)
Allows for multiple layers from different materials

## Slide 50: Extrusion Problems
Melt fracture
Sharkskin or alligator hide
Uneven flow and surging
Degradation
Poor mixing
Contamination
Bubbles in extrudate

## Slide 51: Melt Fracture
Laminar flow or turbulent flow
Material Flow
Die
Material
Material

## Slide 52: Sharkskin or Alligator Hide
Uneven or poor surface finish

## Slide 53: Poor Mixing
Streaks of coloration
Particles

## Slide 54: Bubbles in the Extrudate
Excessive moisture
Absorbed volatiles
Severe degradation in the presence of moisture
  PET, PC, Nylon
Air entrapment

## Slide 55: Thank You