## Slide 1: Foaming
MFG 355

## Slide 2: Foaming Overview
Processes to create foams
  Mechanical, Chemical, Physical, Syntactic (hollow spheres)
  Open and closed cell foams
  Flexible and rigid foams
Processes to shape and solidify foams
  Molding, RIM, Foam-in-place, Extrusion, Casting, Expanded foam molding
Rebond materials
Foam product characteristics

## Slide 3: Foaming
Mechanical foaming
  Mix air into the resin while in a liquid state
  Plastisols, vinyl esters, urea formaldehydes, phenolics, polyesters

## Slide 4: Foaming
Mechanical foaming
  Mix air into the resin while in a liquid state
  Plastisols, vinyl esters, urea formaldehydes, phenolics, polyesters
Polyester foam
Phenolic foam
Phenolic foam

## Slide 5: Foaming
Chemical foaming
  Foaming agents or blowing agents
  Chemical reaction that forms a gas/vapor
Bread (yeast foam)
Urethane foam

## Slide 6: Urethane Foam
Polymerization reaction creates CO2
  The first step reacts isocyanate with water (instead of with a polyol as in a standard urethane reaction)
  The first product is unstable and decompostes
  This causes foaming as the polymer is formed
Polyurea

## Slide 7: Foaming

## Slide 8: Foaming
Physical foaming
  Gas is forced into a liquid or molten resin
  Pressure is released quickly
  Foam is created
Shaving cream

## Slide 9: Foaming
1998 World Cup Soccer Ball
Featured a newly engineered hi-tech syntactic foam layer. This new foam material had better compression and more explosive rebound characteristics, making the ball softer and faster than its predecessor, Questra.
Syntactic foams
  Physically mix in hollow beads
  Beads are usually glass or plastic
  Wide density capability
Glass micro-balloons in epoxy
Interesting Application

## Slide 10: Thermoplastic Microspheres
Syntactic foam with another advantage
  Thermoplastic beads (acrylic, acrylonitrile, polyvinylidene chloride, etc.)
  Filled with low-boiling liquid (isobutene, isopentane)
  Heated to expand

## Slide 11: Open Cell Foams
Open cell foams
  Cells are interconnected
  Air will pass through the foam structure
  Uses
    Cushions
    Filters

## Slide 12: Closed cell foam
Each cell is independent
  Cells don’t interconnect with other cells
  Cells can hold a gas
Uses
  Life vests (or any other water-contact application)
  Cups, plates, etc.
  Insulation

## Slide 13: Processes
Molding
RIM
Foam-in-place
Extrusion
Casting
Expanded foam molding (EPS)
Rebond

## Slide 14: Foam Molding
Foam Inlet
Expandable Mold
Liquid Resin with
Foaming Agent
Fill Position

## Slide 15: Foam Molding
Foam Inlet
Expandable Mold
Liquid Resin with
Foaming Agent
Expanded Position

## Slide 16: Molding and cell structure
Conversion from closed cell to open cell
  Faster expansion
  Higher temperature

## Slide 17: Molded foams

## Slide 18: Reaction Injection Molding
Foaming Agent
Foamed
Part
Mold
In-line
Mixer
Resin
Part A
Resin
Part B

## Slide 19: RIM

## Slide 20: Foam-in-place
Refrigerator Walls
Foam
Foaming Injector
Nozzle

## Slide 21: Extrusion Foaming
Paper
Paper
Extruder
(Resin and Foaming
Agent)
Saw
Belt Drive
Expanded Foam

## Slide 22: Extrusion foam line

## Slide 23: Casting Foams
Resin and
Foaming Agent
Expanded
Foam
Open Pan

## Slide 24: Casting Foams
Skiving the Foamed Bun

## Slide 25: Foam Spraying
Foaming agents mixed as they exit the spray nozzle

## Slide 26: The Foam Test
AFFF system at Ellsworth AFB
Was only supposed to last a few seconds
System wouldn't shut off…
I’d hate to have to explain this.

## Slide 42
Firefighter trying to get the doors open

## Slide 45
Buddle parked this truck here

## Slide 46
Buddle forgot to close the windows
when he parked the truck!!

## Slide 48: Expanded Foam Molding
PS is the standard material used
Can be done with PP or PE as well

## Slide 49: Expanded Foam Molding
Tiny Beads
Expansion
Chamber
Storage
Part
Mold
Steam or Hot Air
Steam or Hot Air
Unexpanded
Expanded

## Slide 50: EPS beads

## Slide 51: EPS

## Slide 52: Rebond
Scrap from other foaming processes
Ground/chopped up
Molded into sheets

## Slide 53: Material Considerations for Foamed Parts
Most thermoplastic and thermoset materials can foamed by one or more of the methods
The most commonly foamed resins are PVC, Polyurethane, PS, PE, PP, Epoxy Phenolic, ABS, Ureaformaldehyde, Silicone, Ionomers and Cellulose Acetates

## Slide 54: Foam Applications
Strength to weight ratios
Thermal insulation (Celestia product)
Energy absorption
Load bearing

## Slide 55: Energy Transmitted
Energy (g's)
Frequency (Hz)
Natural vibration frequency
Truck = 4-6, 12-14/ Train = 2-7, 50-70/ Ship = 2-20; Airplane = 1-3, 25-200

## Slide 56: Load bearing
Polyurethane foam
Natural rubber foam
Vinyl foam
Strain
Stress

## Slide 57: Compression Set

## Slide 58: Thank You