## Slide 1: Compression and Transfer Molding
MFG 355

## Slide 2: Compression Molded Parts
Mold
Part

## Slide 3: Compression Molding

## Slide 4: Compression Molding

## Slide 5: Process Overview
Charge is placed in cavity of matched mold in the open position
Mold is closed by bringing the two halves together
Pressure is exerted to squeeze the resin so that it fills the mold cavity
While under pressure the mold is heated which cures the resin
  Thermosets

## Slide 6: Mold Closure Types
  Flash
Part
Upper
Mold
Lower
Mold
Horizontal
Flash

## Slide 7: Mold Closure Types
Part
Upper
Mold
Lower
Mold
Small Gap
(no flash)
  Positive

## Slide 8: Mold Closure Types
Part
Upper
Mold
Lower
Mold
Horizontal Land
Separated Flash
  Semi-positive

## Slide 9: Materials
Standard thermosets of various types
Molding compounds (mixtures of materials)
  Thermoset resin (30%)
  Reinforcement fibers (10%)
  Fillers (60%)
Bulk Molding Compound (BMC)
Sheet Molding Compound (SMC)

## Slide 10
Bulk Molding Compound

## Slide 11: SMC Parts

## Slide 12
SMC Equipment

## Slide 13: SMC Equipment

## Slide 14: SMC Machine

## Slide 15: Sheet Molding Compound
Charge is made up from thermoset materials
Charge is rolled flat
Multiple layers of SMC can be used in a mold
Longer fibers than BMC

## Slide 16: Compression Machines

## Slide 17: Force Required
  Total force needed per part is determined by:
    Projected area of the part (A)
    Required cavity pressure for the resin (PA)
    Pressure factor that accounts for depth (ρ)
    Depth in excess of the minimum amount (de)
F = (A) [(PA) + (ρde)]

## Slide 18: Compression Molding
Compression molding machines
  Total force that can be exerted is called:
    Press capacity
    Machine rating
    Machine size
    Rated in Newtons or Tons
  Determined by the area of the hydraulic ram and the hydraulic pressure in the line
Press Capacity (tons) =
Area of Ram (inches2) X Hydraulic Pressure (psi)
2000 (pounds/ton)

## Slide 19: Compression Molding vs Injection Molding
Compression Molding
Injection Molding
Cooled mold
Thermoplastic material
Short cycle time (seconds)
Can reprocess flash and waste parts
High part complexity
Undercuts are possible
Uses sprue and runners
Some reinforcement material possible, must be short (whisker length)
Heated mold
Thermoset material
Long cycle time (minutes)
Can’t recycle flash or waste parts
Low part complexity
No undercuts
No sprue or runners
Reinforcement material can be long (inches)

## Slide 20: Transfer Molding
Mixed resin is placed in the transfer chamber
Resin is heated to liquid state
Plunger presses liquid resin through sprue and runner system to mold cavities
Mold is heated
After resin is cured, parts are removed

## Slide 21: Transfer Molding

## Slide 22: Injection Transfer Molding

## Slide 23: Product Considerations
Practically all thermosets can be compression or transfer molded
  Liquids
  Pastes
    Liquid resin with filler
  Doughs
    Pastes with reinforcement
  Granules
    B-staged resin (phenolics)
  Preforms
    Granules pressed into a pre-measured shape for easier handling

## Slide 24: Thermoplastic Compression Molding
Recycling restrictions on European automakers
Strong push for thermoplastics
Attempts to retain molding operations

## Slide 25: Cold Forming, Sintering and Ram Extrusion
Used where heat processing is difficult or impossible
High pressures
Lower temperatures

## Slide 26: Thank You