## Slide 1: Reinforced Plastics
MFG 355

## Slide 2: Advanced Composites
Long (continuous) fibers
Very high performance reinforcements
  Carbon and aramid
Resins are also very high performance
Typically aerospace applications

## Slide 3: Engineering Composites
Shorter fibers/fiberglass
Lower mechanical properties (stiffness)
Lower performance resins

## Slide 4: Reinforcements
Three main types of fibers
  Fiberglass
  Carbon fiber or Graphite
  Organic fibers, aramids (kevlar)

## Slide 5: Reinforcement Forms
Fiber manufacturers package the fibers on spools called tows
Fibers are generally converted to other forms after manufacturing
  Chopped fibers (including whiskers)
  Mat (random)
  Woven fibers
  Tapes
  Prepregs

## Slide 6: Manufacturing Methods
Thermoplastic processes using short fibers
  Injection molding
  Extrusion
  Minor changes are made to accommodate the fiber reinforcements
    All gaps in flow path should be increased
    A resin viscosity decrease may be necessary

## Slide 7: Manufacturing Methods
Matched die or Compression molding
  Reduced flow path over injection or extrusion
  SMC compression molding allows for continuous fibers, mats or weaves
  These processes offer parts that are finished on both sides where most other composite processes do not

## Slide 8: Manufacturing Methods
Resin transfer molding
  Fiber preform is placed in the mold cavity
  Preform doesn’t move—resin is pulled/pushed in

## Slide 9: RTM

## Slide 10
Schematic of a Typical RTM Process
Vacuum
Pressure
Resin Trap
Vacuum
Tooling/Matched Die Mold
Composite Preform
Resin Source
Resin Flow

## Slide 11
Schematic of a Typical RTM Process
Vacuum
Pressure
Resin Trap
Vacuum
Tooling/Matched Die Mold
Composite Preform
Resin Source
Resin Flow

## Slide 12
Schematic of a Typical RTM Process
Vacuum
Pressure
Resin Trap
Vacuum
Tooling/Matched Die Mold
Composite Preform
Resin Source
Resin Flow

## Slide 13
Schematic of a Typical RTM Process
Vacuum
Pressure
Resin Trap
Vacuum
Tooling/Matched Die Mold
Composite Preform
Resin Source
Resin Flow

## Slide 14: VARTM
Vacuum assist resin transfer molding
Using vacuum and not positive pressure
Can use less sturdy molds
May have bagging materials on one side

## Slide 15
Typical VARTM Process Setup
Resin Supply
Distribution Media
Vacuum Bag
Resin Trap
Vacuum
Degas
Vacuum
Porous Release Film
Tool
Sealant
Tape
Preform
Resin
Flow

## Slide 16
Typical VARTM Process Setup
Resin Supply
Distribution Media
Vacuum Bag
Resin Trap
Vacuum
Degas
Vacuum
Porous Release Film
Tool
Sealant
Tape
Preform
Resin
Flow

## Slide 17
Typical VARTM Process Setup
Resin Supply
Distribution Media
Vacuum Bag
Resin Trap
Vacuum
Degas
Vacuum
Porous Release Film
Tool
Sealant
Tape
Preform
Resin
Flow

## Slide 18
Typical VARTM Process Setup
Resin Supply
Distribution Media
Vacuum Bag
Resin Trap
Vacuum
Degas
Vacuum
Porous Release Film
Tool
Sealant
Tape
Preform
Resin
Flow

## Slide 19
Typical VARTM Process Setup
Resin Supply
Distribution Media
Vacuum Bag
Resin Trap
Vacuum
Degas
Vacuum
Porous Release Film
Tool
Sealant
Tape
Preform
Resin
Flow

## Slide 20
Typical VARTM Process Setup
Resin Supply
Distribution Media
Vacuum Bag
Resin Trap
Vacuum
Degas
Vacuum
Porous Release Film
Tool
Sealant
Tape
Preform
Resin
Flow

## Slide 21: Resin Film Infusion (RFI)
Uses layers of film resin with layers of preforms
Assembly is bagged and heated

## Slide 22
Layered RFI
Resin film layer
Fiber preform layer
Vacuum bag
Tool

## Slide 23
T1 (Resin flows and infuses preform)
T2 (Consolidation under pressure)

## Slide 24: Manufacturing Methods
Spray-up
  Fibers are chopped, coated with resin and sprayed onto the mold

## Slide 25: Manufacturing Methods
Hand Lay-up (wet)

## Slide 26: Manufacturing Methods
Hand Lay-up (prepreg)

## Slide 27: Fiber Orientations
Isometric materials have equal strength in all directions
Composites can be lighter weight by not having strength in the directions that it is not needed
Lay-up still has to have some balance and symmetry

## Slide 28: Vacuum Bagging
Provides for increased part consolidation
Reduces matched die mold costs

## Slide 29: Vacuum bagging

## Slide 30: Vacuum bagging

## Slide 31: Vacuum bagging

## Slide 32: Vacuum bagging

## Slide 33: Vacuum bagging

## Slide 34: Vacuum bagging

## Slide 35: Manufacturing Methods
Filament winding and fiber placement
  Fiber placement has greater accuracy
  Fiber placement can wind on less symmetrical and even partially concave mandrels
Tubes, tanks, wind turbine blades and rockets

## Slide 36: Manufacturing Methods
Roll wrapping
  Faster than filament winding
  Limited to symmetrical mandrels

## Slide 37: Manufacturing Methods
Pultrusion
  High volume production
  Comparable to extrusion but the main processing force is tension
  Profile is pulled from the machine

## Slide 38: Manufacturing Methods
Advanced thermoplastic composites
  Difficulties with resin wet-out of the fibers
  High viscosity of the resin
  High temperature for processing

## Slide 39: Advanced Thermoplastics
All highly aromatic
Most common types:
  Thermoplastic polyimides (TPI, PAI, PEI, PBI)
  Polyetheretherketone (PEEK, and related)
  Sulfone and related (PSU, PAS, PES, PPS)
  Liquid crystal polymers (LCP)
  Fluoropolymers (PTFE, PVDF)

## Slide 40: Thermoplastic − Thermoforming
Blanks
Oven
Clamp
Clamping
Pressing
Press (in two modes)
Finished
Part

## Slide 41: Glass Mat Thermoplastic Compression Molding

## Slide 42: Plant Concepts
Many of the processes require considerable space
Curing equipment for large parts can be very large (and expensive)
Controlling volatiles (solvents and resins) must be taken care of
Molds can be both expensive and fragile

## Slide 43: Thank You