## Slide 1: Fundamentals of Composites Manufacturing Materials, Methods, & Applications
Chapter 10 : Quality and Testing

## Slide 2: Chapter 10: Quality and Testing - Overview
History of composite materials testing
Quality control principles
Component materials testing
Mechanical testing
Thermal and environmental testing
Flammability testing
Non-destructive testing and inspection

## Slide 3: History of Composite Materials Testing
Factors explaining the lack of accepted composited data
  The complexity of composites
  The relative newness of composites as materials
  The continuous development of new composites
  The scarcity of standardized tests for composites

## Slide 4: Quality Control Principles
Quality is a process, not a destination.
5 primary functions that quality tools are to address
  Documentation and certification programs
  Analysis and statistical tools
  Improvement methods
    FMEA, Cause-and-effect diagram, QFD, Benchmarking, Taguchi loss function
  System integration strategies
  Management philosophies

## Slide 5: Quality Control Principles
Figure 10-1 Correlation plot of hardness versus temperature

## Slide 6: Quality Control Principles
Figure 10-2 Histogram

## Slide 7: Quality Control Principles
  Figure 10-3 Pareto chart

## Slide 8: Component Material Testing
Figure 10-4 Viscosity measuring equipment

## Slide 9: Component Material Testing
Raw Material Testing
  Drape test
  Tack Test
Curing Tests
  DSC

## Slide 10: Mechanical Testing
Figure 10-5 Types of forces

## Slide 11: Mechanical Testing
Table 10-1 Mechanical properties of a typical carbon-epoxy composite

## Slide 12: Mechanical Testing
Figure 10-6 Tensile test specimens

## Slide 13: Mechanical Testing
Figure 10-7 Relationships of the tensile strength of fiber, matrix, and composite.

## Slide 14: Mechanical Testing
Tensile Testing
  Relationship between stress and strain
    F/A = σ = Eε
    where:
      F = Force
      A = cross-sectional area
      σ = stress
      ε = strain
      E = modulus or Young’s modulus

## Slide 15: Mechanical Testing
Tensile Testing
  Burst Test
  Open-hole tensile test
Compression and Compression-After-Impact Properties

## Slide 16: Mechanical Testing
Figure 10-8 flexural test

## Slide 17: Mechanical Testing
Figure 10-9 Simple peel test

## Slide 18: Mechanical Testing
Figure 10-10 Rolling drum peel test

## Slide 19: Mechanical Testing
Figure 10-11 Izod and Charpy impact tester and specimens

## Slide 20: Mechanical Testing
Figure 10-12 Creep test

## Slide 21: Mechanical Testing
Creep
  σ0 = E(t,T)ε(t,T)
    Where:
      σ0 = applied stress (usually a constant)
      E = creep modulus
      ε = amount of deformation (strain due to creep)

## Slide 22: Mechanical Testing
Creep
  Methods used to reduce creep
    Orient fibers in directions of highest loads
    Increase the fiber content
    Select high-modulus fibers (increase stiffness)
    Reduce the stress level
    Reduce the temperature
    Utilize initial loading cycles

## Slide 23: Mechanical Testing
Fatigue
  Composites tend to stabilize early in fatigue loading through the following mechanisms:
    Matrix micro-cracking
    Blunting of cracks at the fiber surface
    Delaminations between layers
    Stress redistribution and load sharing
    Energy dissipation from visco-elastic effects of the matrix

## Slide 24: Mechanical Testing
Figure 10-13 Fatigue testing for various materials

## Slide 25: Mechanical Testing
Vibration and Damping
  Constrained layer damping
  Active damping
  Stress-couples activated damping

## Slide 26: Thermal and Environmental Testing
Temperature Effects
  Coefficient of thermal expansion (CTE)
  Table 10-2 Representative coefficients of thermal expansion for epoxy-matrix composites

## Slide 27: Thermal and Environmental Testing
Figure 10-14 Specific strength as a function of temperature

## Slide 28: Thermal and Environmental Testing
Table 10-3 Moisture and absorption for neat (non-reinforced) resins

## Slide 29: Thermal and Environmental Testing
Figure 10-15 Fiberglass-epoxy exposure to various moisture conditions

## Slide 30: Thermal and Environmental Testing
Aging and Service Life Considerations
  Suggestions for establishing a basis for predicting service life:
    Define the service environment in terms of exposure time, temp, humidity, and loading conditions
    Review the database after selecting materials to see what is already known about them
    Conduct accelerated aging tests on the materials
    Accelerated aging analysis
    Verify the data

## Slide 31: Flammability Testing
Understand How Composites Burn
Combustion Characteristics of Organic Resins and Plastics
  Properties considered when examining the burning of composites/plastics
    Ease of ignition/flame resistance
    Flame spread/fire-retardant properties/surface flammability
    Heat release rate
    Fire endurance
    Ease of extermination
    Smoke emission/toxicity
    Physical characteristics

## Slide 32: Flammability Testing
Types of Flammability Testing
  Test Categories
    Official tests
    Laboratory tests
    Full-scale tests

## Slide 33: Flammability Testing
Table 10-4 Summary of fire requirements for composite materials in the US.

## Slide 34: Flammability Testing
Figure 10-16 Limiting oxygen index test

## Slide 35: Non-Destructive Testing and Inspection
General Principles
  Sending an energy signal (wave) through or onto the part and then detecting changes in that signal compared to some standard.
Ultrasonic Testing
Acoustic Emission
Radiography
Thermography
Optical Holography
Microwave Frequencies
Eddy Current
Visual Inspeciton